Technical Data Sheet

| No | CHARACTERISTIC | NW013 | NW035 |  | NW058 |  | METHOD |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Appearance | Colorless or white or almost white mass; the melted substance is free from fluorescence in daylight |  |  |  | BP 2022 |  |
| 2 | Odor | Odorless |  |  |  |  | - |
| 3 | Oil content % | 1-3 |  | 3-5 | 5-8 |  | ASTM D-721 |
| 4 | Kinematic Viscosity @100 ͦ C | 6-8 cSt |  | 6-8 cSt | 6-8 cSt |  | ASTM D-445 |
| 5 | Color Lovibond | 0.1_0.5 Y |  | 0.2_0.6 Y | 0.5_1 Y |  | IP 17 cell 2" |
| 6 | Drop Melting Point | 60-70 ͦ C |  | 60-70 ͦ C | 60-70 ͦ C |  | ASTM D-127 |
| 7 | Congealing point | 60-70 ͦ C |  | 60-70 ͦ C | 60-70 ͦ C |  | ASTM D-938 |
| 8 | Needle Penetration (0.1mm) | 1_5 |  | 5_15 | 10_20 |  | ASTM D-1321 |

Semi Refined Paraffin Wax